Code No:222103

Set No.

1

II B.Tech.II-Semester Supplementary Examinations November-2003

AEROSPACE MATERIALS

(Aeronautical Engineering)

Time: 3 hours							Max. Marks: 80

Answer any FIVE questions

All questions carry equal marks

---

1.a)	What are the various machines/methods used for testing the hardness of a material?  How will you perform the following tests and what are their advantages and disadvantages.

(i)	Brinnell Hardness Test		(ii)	Vicker’s Hardness Test

b)	Explain the phenomenon of strain hardening.  How it is carried out?  Show the effect of strain hardening on steel/copper with the help of a neat sketch.

2.	What is SAE numbering system to classify the steels?  Explain the percentage of alloying elements, properties and application of the following steels.

(i)   SAE 1025	     (ii)	SAE  2320   (iii)   SAE  3115	     (iv)	SAE   4130

3.a)	How do you classify wrought aluminium alloys?  Explain briefly about the classifications.

b)	Write short notes on the following with respect to alluminium alloys.

(i)	Alclad aluminium alloys		(ii)	Die casting

- Corrosion resistance			(iv)	Permanent mold casting

4.	Why magnesium alloys are important in the field of aeronautics?  What are the various forms of magnesium alloys available?  Explain the reasons for limited use of magnesium alloys in aeronautical field.  List various applications.

5.a)	What do you understand by composites?  List down the advantages and disadvantages of composites over traditional metallic material.

b)	How various composite materials can be stored?  Explain.

6.a)	What is a bonded structure?  Classify various type of bonded structures.

b)	How can you test bonded structural joints for crack or delamination?  Explain two methods for effectively testing the bonded joints.

7.a)	Explain the various types of glasses along with  their uses in aircraft industry?  How testing of the glass (nonscatterable) is carried out?

b)	How quality affects the construction of honeycombs?  Explain.

8.	Write short notes on the following:

a)	K-Monel				b)	Forging of super alloys

- Bauchinger’s effect of matches	d)	Diffusion Bonding.

&&&

Code No:222103

Set No.

2

II B.Tech.II-Semester Supplementary Examinations November-2003

AEROSPACE MATERIALS

(Aeronautical Engineering)

Time: 3 hours							Max. Marks: 80

Answer any FIVE questions

All questions carry equal marks

---

1.a)	Explain the factors affecting the choice of materials for the construction of important aircraft parts.

b)	Explain linear and non-linear elastic properties of a typical material with the help of a stress-strain curve.  Also explain the Elastic after effect.

2.a)	Which features of Titanium make it important in the field of aeronautical industry?  hat are its alloying capabilities?  List few applications of titanium alloys in aeronautical field.

b)	How Titanium alloys are heat treated.  Which factors affect the working properties of Titanium alloys after heat treatment?

3.a)	Explain the effect of alloying elements on cast iron.

b)	What do you understand by Maraging steels?  Explain the properties and applications of maraging steels in aerospace industry.

4.a)	How do you classify corrosion resistant steels?  Which type of corrosion affects the corrosion resistant steels and how corrosion can be prevented?

b)	What are the factors affecting the strength of wood?  Explain few application of wood in aeronautical field.

5.a)	What are the important properties of honeycomb structures?  How these structures are prepared?

b)	What are bonded structures?  List the various advantages of bonded structures?  How bonded structures help in weight saving and crack arresting?

6.	Explain and classify the composite materials.  Explain the process of fabrication of composite materials.

7.a)	What are the characteristics of composites?

b)	Write a descriptive note on ‘Adhesive materials’ for bonded structures.

8.	Write short notes on the following:

a)     Monel			  b)    Bonded sandwich structures

c)   Alclad aluminium alloys	  d)   Heat treatment of aluminium alloy rivets.

&&&

Code No:222103

Set No.

3

II B.Tech.II-Semester Supplementary Examinations November-2003

AEROSPACE MATERIALS

(Aeronautical Engineering)

Time: 3 hours							Max. Marks: 80

Answer any FIVE questions

All questions carry equal marks

---

1.a)	What do you understand by ‘hardness numbers’?  Explain various types of hardness numbers.

b)	How will you test an aircraft component for flaw detection?  Explain one destructive and one non-destructive testing technique.

2.a)	Which magnesium alloys are used in an aeroplane structure?  What are their advantages?  Where are these alloys used in an aeroplane structure?

b)	Explain briefly the working properties of titanium alloys.

3.	Write a short note on alloy steels and explain in detail the effects of the following elements on alloy steels.

(a)  Carbon	b) Nickel    c)  Silicon      d) Manganese    v)  Chromium

4.a)	Why high strength to weight ratio is important in case of aircraft.  List the materials which have the high strength to weight ratio.

b)	What do you understand by super alloys?  Explain the broad categories of super alloys.

5.a)	Explain the working properties and applications of rubber in aeronautical field, of rubber.  Classify the rubbers.

b)	Explain the phenomenon of crack arresting in case of bonded structures.

6.	What do you understand by NDT techniques?  Explain various NDT techniques used to detect the flaws, cracks in case of bonded joints.

7.	Explain glass and carbon composites?  Show the use of composites in an advanced fighter aircraft with the help of three views sketch of aircraft.  Explain the reason of usage of particular material for a particular component.

8.	Write short notes on the following:

(a)      Costing of composites		(b)   Inconel

(c)    SAE 6150			(e)   Shot welding of aluminium alloy.

&&&

Code No:222103

Set No.

4

II B.Tech.II-Semester Supplementary Examinations November-2003

AEROSPACE MATERIALS

(Aeronautical Engineering)

Time: 3 hours							Max. Marks: 80

Answer any FIVE questions

All questions carry equal marks

---

1.a)	Explain the following methods/machines for testing the hardness of the material (i)   Rockwell Hardness Test		(ii)	Shore Scleroscope

Also state the advantages and disadvantages of the above machine.

b)	Explain briefly the elastic properties of a typical ductile material with the help of a stress-strain curve.

2.a)	Explain various desirable properties of  aerospace materials.

b)	Explain the percentage of alloying elements, properties and applications of the following steels.

(i)	SAE 1095	(ii)	SAE  2330   iii)   SAE  3140	(iv)       SAE   4140

3.a)	Write in detail on the following:

(i)	Carbon-Carbon composites		(ii)	Metal matrix composites

b)	How costing of composites affects the usage of composites in aircraft structures.  Compare it with metallic structures.

4.a)	Explain briefly the factors contributing to the corrosion of magnesium alloys.  What are the specials treatments adapted to prevent the magnesium alloys from corrosion?  Explain briefly.

b)	Write short note on ‘Vulcanizing’.

5.a)	How super alloys are heat treated?  Explain various processes.

b)	What are the desirable features/properties of the plastics to be used in aircraft?  Explain various types of plastics along with their uses.

6.a)	Explain desirable properties and various types of glues briefly.

b)	What re the distinguishing features of aluminium alloys?  How the heat treatment of aluminium alloys is carried out?

7.a)	What are the advantages of Bonded structures in airframe?

b)	Explain the method of construction of honeycomb structures.

c)	Write a short note on ‘Diffusion Bonding’.

8.	Write short notes on the following:

(i)	Testing of composites			(ii)	Welding of super alloys

- Casting of magnesium alloys

- Corrosion and corrosion prevention of titanium alloys.

&&&