Code No: 310604

Set No.

1

IV-B.Tech. I-Semester Supplementary Examination, June 2003

METALLURGICAL THERMODYNAMICS

(Metallurgy and Material Technology)

Time: 3 hours							Max. Marks: 80

Answer any Five questions

All questions carry equal marks

- - -

1.a)	A steel tank contains hydrogen at a constant pressure of 10atm with a vacuum out 	side. The hydrogen concentration at the inner surface of the tank is 10kg/m3. 	DH2 at R.T in steel is 10-9m2/s. Calculate the rate at which H2 escapes through 	the wall of tank which has a thickness of 5mm.

b)	Describe Kirkendal effect in diffusion.

c)	Explain diffusion along grain boundaries and surfaces.

2.a)	Explain variation of equilibrium constant with temperature and derive van’t Hoff 	equation.

b)	Calculate H0 and S0 at 298K for the reaction; 2Cu(S) + ½ O2(g) ⇌ Cu2O(S) 	G0 = -169452 - 16.4 T log T + 123.45 T Joules.

3.a)	Explain the specific heat of solids and Einstein model of the lattice.

b)	Explain thermal expansion and lattice thermal conductivity.

4.a)	Explain determination of partial modal quantities from integral molar quantities.

b)	Explain Sievert’s law and excess thermo dynamics properties.

5.a)	Derive Gibb’s phase rule and apply it to entectic point of binary alloy system.

b)	Explain determination of solidus and liquidus lines for ideal solutions.

6.a)	What is standard electrode potential. Distinguish electro - chemical cells from 	galvanic cells.

b)	Explain determination of thermodynamic properties from electro - chemical cells.

7.a)	Classify the defects in solids.

b)	Derive an equation for equilibrium concentration of point defects as a function of 	temperature.

c)	Calculate the ratio of the number of vacancies in equilibrium at 300K in Al to that 	produced by rapid quenching from 8000K.

8.	Write short note on the following:

a)	Determination of intrinsic diffusivities.

b)	Use of Oxygen monograms in Ellingham diagrams.

c)	Thermo - electric effects.

d)	Actual (non ideal ) solutions.

~ ~ ~ ~

Code No:310604

IV-B.Tech. I-Semester Supplementary Examination, June 2003

Set No.

2

METALLURGICAL THERMODYNAMICS

(Metallurgy and Material Technology)

Time: 3 hours							Max. Marks: 80

Answer any Five questions

All questions carry equal marks

- - -

1.a)	Derive Fick’s law of diffusion under steady state.

b)	Describe Matano method of diffusion.

c)	Explain temperature dependence of the diffusion co-efficient.

2.a)	Derive and explain uses of the Oxygen nomographic scale in Richardsons 	diagrams.

b)	Calculate the equilibrium constant for the reaction.

Ni (s) + H2 (g) = Ni (s) + H2O (g)

at 7500C from the following data

Ni (s) + ½ O2 (g) = Ni O (g)

G0 = - 58,450 + 23.55 T  cal.

H2 (g) + ½ O2 (g) = H2O (g)

G0 = - 58,900 +  13.1 T  cal.

3.a)	Calculate the temperature if 12000 calories are introduced 500gms of a material at 	300C which has a specific heat of 0.03 cal / g.k.

b)	Explain thermal expansion and thermo - electric effects.

4.a)	Prove that:

(i)	ΔHmXS=ΔHm and

(ii)	RT ln γi is a constant for a regular solution.

b)	Derive Gibbs - Duhem equation for a solid solution.

5.a)	Explain equality of chemical potentials in equilibrated phases and determination 	of phase diagrams.

b)	Derive Gibb’s phase rule and explain determination of liquidus for ideal 	solution.

6.a)	Define decomposition voltage and over voltage. Derive an equation for 	standard electrode potential.

b)	From e.m.f. measurements, the activity co-efficient of aluminium in liquid iron-	aluminium  alloys at 16000C is given by:

logγA1=2.60NA1−1.51

calculate the activity of iron in 90% iron alloy at this temperature.

(Contd…)

Code No: 310604.			.. 2 ..				Set No: 2

7.a)	Explain types of point defects.

b)	What are line and surface defects.

c)	The enthalpy  of formation of a frenkel defect ΔHfFr  in AgCl is 1.4 e.v.  Calculate the ratio of the number of Frenkel defects at 250C to that obtained by rapid cooling after holding at 3000C.

8.	Briefly write on any three of the following:

a)	Determination of intrinsic diffusivities.

b)	Use of Oxygen nomograms in Ellinghan diagrams.

c)	Ideal solutions.

d)	Concentration cells.

~ ~ ~ ~

Code No: 310604

IV-B.Tech. I-Semester Supplementary Examination, June 2003

Set No.

3

METALLURGICAL THERMODYNAMICS

(Metallurgy and Material Technology)

Time: 3 hours							       Max. Marks: 80

Answer any Five questions

All questions carry equal marks

- - -

1.a)	Derive Fick’s law of diffusion under un-steady state.

b)	Explain diffusion along grain boundaries and free surfaces.

c)	Describe determination of intrinsic diffusivities.

2.a)	Describe Ellingham diagrams in general and their applications.

b)	A steel bath at 16000C contains 0.005% N2 and 10 ppm of H2. Calculate the equilibrium partial pressure of these elements in the gases evolved in the boil. Given that the solubility of N2 at 16000C is 0.04 wt% and that of H2 is 0.0027 wt%.

3.a)	Explain Einstien and Debyees model of the lattice.

b)	Explain an harmonicity and thermo electric effects.

4.a)	What is the significance of partial molal quantities and explain determination of one partial molal quantity from another.

b)	What are the properties of ideal solutions? What is Henry’s law?

5.a)	Derive Gibb’s phase and apply it entectic temperature of a binary system.

b)	Explain determination of liquids for entectic system.

6.a)	Explain the application of Gibb’s-Helmholtz equation to galvanic cells.

b)	What is meant by polarization and over voltage? Derive Nernst equation for single electrode potential.

7.a)	Distinguish between Frenkel and Schotky defects.

b)	Explain surface defects.

c)	Calculate the number of vacancies per cubic centimeter in copper at 250C if 20,000 cals/mole are required to produce a vacancy in copper. acu = 3.62A0.

8.	Write short notes on any three of the following:

a)	Temperature dependence of diffusion co-efficient.

b)	Nomographic scale in Richardsons diagram.

c)	Excess thermodynamic quantities.

d)	Concentration cells.

~ ~ ~ ~

Code No: 310604

IV-B.Tech. I-Semester Supplementary Examination, June 2003

Set No.

4

METALLURGICAL THERMODYNAMICS

(Metallurgy and Material Technology)

Time: 3 hours							    Max. Marks: 80

Answer any Five questions

All questions carry equal marks

- - -

1.a)	Derive the Darken’s equations.

b)	Explain temperature dependence of the diffusion co-efficient.

c)	Describe Self diffusion in pure metals.

2.a)	Explain relation between standard free energy change and equilibrium constant.

b)	Determine equilibrium constant at 800K for NH3 synthesis reaction given that:

H0 298 K = - 46,190 J / gm / mol.

G0 298 K = - 16,635 J / gm / mol.

Cp0          =  - 31,780 + 35.517  x  10-3 T

- 9.316  x  10-6 T2  J / gm - mole / k.

3.a)	Calculate the temperature if 14000 calories are introduced to 500gms of a material 	at 280C which has a specific heat of 0.027 cal/g.k.

b)	Explain thermal conductivity and thermo -electric effects.

4.a)	Prove that for a dilute solution the solvent follows Raoult’s law where the solute 	obeys Henry’s law.

b)	Explain integration of Gibb’s Duhem equation.

5.a)	Explain concept of chemical potential and determination of phase diagram.

b)	Derive Gibb’s phase rule and explain determination of solidus for entectic 	system.

6.a)	Show the variation of chemical potential of a component i  with pressure p is 	given by:

d  i = Vi , m . dp

b)	Explain determination of thermodynamic quantities from electro- chemical cells.

7.a)	Classify the defects in solids and explain surface defects.

b)	Distinguish between Frenkel and shotky defects.

c)	Calculate the ratio of the number of vacancies in equilibrium at 300K in Al to that 	produced by rapid quenching from 700k.

(Contd…)

Code No: 310604.			.. 2 ..					Set No: 4

8.	Write short notes on any three of the following:

a)	Application of Fick’s laws of diffusion.

b)	Nomographic scale in Richardsons diagrams.

c)	Excess thermodynamic quantities.

d)	Galvanic cells.

~ ~ ~ ~