Code No.: 420854

### OR

# IV B.Tech II Semester Examination April 2003

CORROSION ENGINEERING

(Chemical Engineering)

## Time: 3 hours							Max. Marks.70

# Answer any Five questions

All questions carry equal marks

---

1. a)	With the help of dry cell battery analogy, explain the mechanism of corrosion.  Give anodic and cathodic reactions. Give the schematic diagram of such a corrosion cell.

b)	Explain the environmental effects on corrosion rate with reference to effect of velocity.

2. a)	What do you understand by Polarization?  Explain the different types of polarization.

- Discuss about Emf series and galvanic series.

- Explain the beneficial applications of galvanic corrosion.

3. 	Discuss the following:

- Streicher test for stainless steels.

- Test for studying crevice corrosion.

- Planned Interval tests.

4. a)	Discuss about classification of stainless steels giving examples for each.  Bring out the differences in their properties.

b)	What is passivity?  Explain the corrosion characteristics of an active passive metal with reference to passivity.

c)	Name eight forms of corrosion.

5. a)	Explain the comparison between corrosion behavior of Zinc when galvanically coupled to Gold with that of coupling with platinum.  What is the conclusion that can be drawn from this?

- Explain selective Leaching.

- Explain Tafel extrapolation method to determine corrosion rate.

6.	What is crevice corrosion?  What is its mechanism?  Write the methods to combat crevice corrosion?

7. a)	What are different chemical conversion coatings employed commercially?  Describe any one method used for a non-ferrous metal like Aluminium.

- Draw a comparison between Anodic and cathodic protection.

Contd…2

Code No. 420854				.2.				Set: OR

8. a)	‘Metal frequently corrode under a scale deposit or wood when exposed to aqueous solution’.  Justify the statement.

b)	Show with Electrochemical reaction how rust forms on a piece of steel immersed into water.

- The linear polarization slop, E/i at low current density for iron in a corrosive solution is 3.57 mV/mA.cm2.  Calculate the corrosion rate of iron in mdd.  Assume that the Tafel constants are equal to 0.1V.

- What is the Redox potential of copper in 0.02N H2So4 (Ecuo= 0.337 V)

###